K71300 Series Visual Effects Gloss Cast Vinyl Over-Laminating Films A luxury and innovative over-laminate that transforms any application with the creation of a subtle pearlescent sheen. These high quality over-laminating films have been specially developed for use in the digital imaging industry to permanently enhance and protect the printed media. They offer a premium solution to over-laminating applications by using a solvent based acrylic adhesive system. The film is available as:- K71311 K71312 K71313 K71314; Gloss Pearlescent Green Cast Overlaminate Gloss Pearlescent Blue Cast Overlaminate Gloss Pearlescent Indigo Cast Overlaminate Gloss Pearlescent Magenta Cast Overlaminate.

| CHARACTERISTIC | TEST METHOD | TYPICAL VALUE |
| --- | --- | --- |
| Film Thickness | ISO 4591:1992 | 50 micron |
| Adhesive Thickness | ISO 4591:1992 | 25 micron |
| Adhesive Type |  | Clear Permanent Acrylic |
| Release Liner |  | Double Sided PE Liner |
| Storage |  | Two years, out of direct sunlight at 23°C and 50% humidity |
| Tensile | ISO 527:1996 | >13.5 N/mm² |
| Elongation | ISO 527:1996 | >75% |
| Adhesion 20 Mins/180° | FINAT FTM1/Painted Plate | 450 N/Metre |
| Adhesion 24 Hrs/180° | FINAT FTM1/Painted Plate | 530 N/Metre |
| Static Shear (25 x 25mm) | FINAT FTM8/Stainless Steel | >16 hours |
| Dimensional Stability | FTM14/Aluminium | <0.4mm |
| (150 x 150mm/48 hours/70°C) |  |  |
| Gloss 60° | ASTM 523-89 | >85% |
| Flammability |  | Self Extinguishing |
| Artificial Weathering | Atlas Xenon arc | >1000 hours |
| Weathering | Vertical Exposure/Mid Europe | Ongoing |
| Application Temperature | Clean, dry surface | +8°C to 25°C |
| Service Temperature |  | -40°C to +105°C |
| Resistance to various liquids after application and conditioned for 24 hours at 23C. Results examined 1 hour after test. |  |  |
| Humidity | 24 hours at 38°C and 100% | No Effect |
| Water (Distilled) | 24 hours at 32°C | No Effect |
| Sea Water | 1 year Mid Tide (BS 5609:1986) | No Effect |
| Reference Fuel | 1 hour at 23°C | Very Slight Film Softening |
| Diesel Fuel | 1 hour at 23°C | No Effect |
| SAE Motor Oil | 24 hours at 23°C | No Effect |
| Antifreeze/Water (1:1) | 24 hours at 23°C | No Effect |
| Detergent Solution | 8 hours at 65°C | No Effect |
| Hydraulic Oil | 24 hours at 23°C | No Effect |
| Battery Acid | 24 hours at 23°C | No Effect |
| Although we have good control of the colour production at KPMF, it is advisable to avoid using different batches of material for the same end application |  |  |

KPMF films should not be applied to unsound surfaces or to surfaces which may subsequently crack, peel, outgas or are of low surface energy. It is recommended that any application surface should have an energy level in excess of 40 dyne/cm. (Polyolefins should be in excess of 45 dyne/cm). The above data shows typical properties and should not be taken as a guarantee for performance. Purchasers should determine the suitability of each product prior to its intended use. Prolonged exposure to high and low temperatures in the presence of chemicals such as solvents, acids etc. may eventually cause deterioration. Durability is based on middle European exposure conditions. Actual performance will depend on substrate preparation, exposure conditions and application of marking. IMPORTANT Kay Premium Marking Films are produced under stringent manufacturing conditions. The information and typical values shown are based upon research believed to be reliable and are provided without guarantee and do not constitute a warranty. The values are not for use in specifications. Ink and paint systems can affect the performance of film and also the adhesive properties, as can application techniques. Users are advised to ensure that performance and reliability are not compromised by determining the suitability of each product prior to its intended use. WARRANTY Kay Premium Marking Films are produced under careful quality control and are warranted to be fit for the purpose and free from defect in material and workmanship. Any material shown to be defective to our satisfaction at the point of sale shall be replaced free of charge. Kay Premium Marking Films Limited liability to the purchaser shall in no circumstances exceed the cost of the amount of the defective material supplied.